NASA TN D-8093

APOLLO EXPERIENCE REPORT - DEVELOPMENT OF THE

EXTRA VEHICULAR MOBILITY UNIT

Стр. 20

TABLE V . - THERMAL AND OPTICAL PROPERTIES OF THE L EVA

| Parameter | Spectral band wavelength λ, μm |
| --- | --- |
|  | Ultraviolet , to 0.38 | Visible, 0.38 to 0.76 | Near infrared 0.76 to 3.0 | Far infrared, from 3.0 |
| Pressure helmet |
| Reflectance inside, ρ i . | 0.14 | 0.01 | 0.15 | 0.07 |
| Reflectance outside, ρ o | .14 | .01 | .15 | .07 |
| Transmittance, τ | .18 | .92 | .68 | .00 |
| Emittance inside, ɛ i | -- | -- | -- | .93 |
| Emittance outside, ɛ o | -- | -- | -- | .93 |
| Impact protective visor |
| Reflectance inside, ρ i . | 0.13 | 0.07 | 0.50 | 0.90 |
| Reflectance outside, ρ o | .07 | .11 | .37 | .05 |
| Transmittance, τ | .00 | .63 | .37 | .00 |
| Emittance inside, ɛ i | -- | -- | -- | .10 |
| Emittance outside, ɛ o | -- | -- | -- | .95 |
| Sun visor |
| Reflectance inside, ρ i . | 0.08 | 0.04 | 0.66 | 0.94 |
| Reflectance outside, ρ o | .08 | .28 | .58 | .06 |
| Transmittance, τ | .01 | .19 | .12 | .00 |
| Emittance inside, ɛ i | -- | -- | -- | .06 |
| Emittance outside, ɛ o | -- | -- | -- | .94 |